## Slide 1: High-resolution Spin Vectorial Measurement on Spin-orbit Interaction Induced Electronic Structure of Low-dimensional System
Taichi Okuda
Hiroshima Synchrotron Radiation Center,
Hiroshima University

## Slide 2: Outline
Introduction
Spin resolved ARPES
  ESPRESSO machine
2D
  MoS2: Spin and Valley coupling
1D
  Au nanowire on Ni(110): 1D-Rashba + TRS breaking
Summary

## Slide 3: Normal Rashba in ideal 2DEG
Introduction

## Slide 4: Rashba effect on Au(111)
Au(111)
F. Reinert et al., PRB 63 (2001) 115415.
ARPES
Spin-ARPES
M. Hoesch et al. PRB69, 241401(R)(2004).
Introduction

## Slide 5: Deviation from the ideal Rashba effect
Out of plane spin component by warping effect
C. Ast et al., Phys. Rev. Lett. 98, 186807 (2007).
E. Frantzeskakis and M. Grioni, Phys. Rev. B 84, 155453 (2011).
Introduction
Ag2Bi

## Slide 6: Deviation from the ideal Rashba effect
100% out-of-plane spin polarization
by surface structural symmetry (C3)
[1] K. Sakamoto, et al., Phys. Rev. Lett. 102, 096805 (2009).
Si(111)1x1-Tl
Introduction

## Slide 7: Valley spin polarization by extraordinary Rashba on Si
K. Sakamoto et al., Nat. Commun. 4, 2073 (2013).
Valley dependent spin polarization is realized in Rashba surface state
Introduction

## Slide 8: Deviation from the ideal Rashba effect
T. Okuda et al. PRB82, 161410(R) (2010).
J.N. Crain and F. J. Himpsel, Appl. Phys. A 82, 431 (2006).
Rashba effect in 1D electronic states
Au/Si(557)
Introduction

## Slide 9: Deviation from the ideal Rashba effect
Rashba effect in bulk crystal by breaking of bulk inversion symmetry along Z axis
K. Ishizaka et al., Nat. Mater. 10, 521 (2011).
BiTeI
Introduction

## Slide 10: Today topics
Spin and valley coupling in bulk crystal
  3R-MoS2
1D Rashba system on magnetic materials
  (1D-Rashba spin split +Time reversal symmetry breaking)
  Au nanowire on Ni(110)

## Slide 11
Spin- and Angle-resolved photoemission (SARPES) is one of the most suitable tools to explore and/or investigate new systems.
SOI induced spin polarized states (Rashba system, Topological Insulator etc.) have no net magnetic moment.
Observation of spin property by transport measurement is difficult.
Measurement with spin- and k-resolution is indispensable.
As seen in the introduction,

## Slide 12: Spin-resolved ARPES
25 kV
Spin-Orbit Interaction
Electron
Scattering plane
Target (Au, Th etc.)
θ=120°
Quantization axis
Mott scattering
Efficiency is 1/10000
Typical energy and angular resolutions
ΔE~ 100-200 meV, Δθ~±1-2°

## Slide 13: High efficiency spin detector VLEED
M
-M
Fe(001)
film
I+
I-
Spin dependent electron scattering by Ferromagnetic target (Ek~10 eV)
D. Tillemann et al., Z. Phys. B. 77, 1 (1989).
Efficiency of VLEED detector
Electron reflectivity (I/I0) 1/10 (×10)
Effective Sherman func.(Seff) ~ 40 % (×2-4)
Fe(001) film
MgO(001) substrate
Fe(001)p1x1-O
Fe(001) film can be protected by preoxidized surface (Fe(001)p1x1-O)
100 times higher efficiency is realized
Figure of Merit (FOM) 10-2
Lifetime of target is more than a week in UHV

## Slide 14: ESPRESSO machine (Efficient SPin REolved SpectroScOpy)
Apparatuses
Very Low Energy Electron Diffraction (VLEED) spin detector
  FOM = 1.2x10-2
  (100 times higher than Mott)
High-resolution hemispherical analyzer (VG-SCIENTA R4000)
Resolution
  Best
  (DE, Dq)=(7.5 meV, ±0.2°)
  Typical
  (DE, Dq)=(~20 meV, ±0.38~0.75°)
Special function
  Efficient normal ARPES
  3D spin vector observation
  (Px，Py，Pz)
T. Okuda et al., Rev. Sci. Insturm.. 82, 103302 (2011).
J. Electron Spectrosc. Relate. Phenom. 201, 23 (2015).

## Slide 15: Comparison between Mott and VLEED
Surface states of Bi(111) by ARPES
×10
Resolution
SARPES data taken with Mott detector
R. Nishimura., master thesis (2009).
Emission angle(deg.)
Emission angle(deg.)
Binding Energy (eV)
Binding Energy (eV)
Spin-up
Spin-down
SARPES data taken with ESPRESSO machine
T. Okuda et al., Rev. Sci. Insturm.. 82, 103302 (2011).

## Slide 16: Hiroshima Synchrotron Radiation Center (HiSOR) BL-9B
HiSOR
BL9B (APPLE II)
Photon energy
  16-50-(300) eV
  Xe (8.43 eV)
  He (21.22 eV)
Polarization
  Helical
  Vertical
  Horizontal
Quasi periodic
Apple II undulator
Storage ring
0.7 GeV Circumference 21.95 m

## Slide 17: Today topics
Spin and valley coupling in bulk crystal
  3R-MoS2
1D Rashba system on magnetic materials
  (1D-Rashba spin split +Time reversal symmetry breaking)
  Au nanowire on Ni(110)

## Slide 18: Transition Metal DiChalcogenide (TMDC) MCh2
Agnieszka Kuc, Chemical Modelling: 11, pp 1-29 (2014).
MCh2
M:
Ti, Zr, Hf (Group IV)
Nb, Ta (Group V)
Mo,W (Group VI)
Ch: S, Se
Ionicity
Group IV  Octahedral
Group V
Group VI  Trigonal
Covalency

## Slide 19: Spin valley coupling in monolayer group IV dichalcogenides (TCh2 (T=Mo, W, Ch=S, Se))
D. Xiao, G.-B. Liu, W. Feng, X. Xu, and W. Yao, Phys. Rev. Lett. 108, 196802 (2012).
Effective Hamiltonian in kp perturbation for VB top around K-point
Pauli matrix for spin
τ = ±1: Valley index
2λ= spin splitting
Strong spin orbit interaction in d electron
Breaking of in-plane inversion symmetry
Coexistence of
Valley hall effect
Spin hall effect
Zeeman type spin splitting at K point
Spin polarization reversal at K and K’
Top view
Side view
Trigonal structure

## Slide 20
How can we get MoS2 having in-plane inversion symmetry breaking?
2H-MoS2
(P63 /mmc)
1ML MoS2
(P6m2)
Mo
S
3-fold
Mirror
Planes
Noncentro-
symmetric
Centro-
symmetric
Inversion
center
6-fold
3R-MoS2
(R3m)
Mirror Planes
3-fold axis
Noncentrosymmetric
Point group C3v
Spin-Valley
coupling in bulk
x
z
Mo
S
S

## Slide 21: Crystal growth and characterization
Screw dislocation of 2H and 3R sample
Electron diffraction pattern of 2H and 3R sample
6mm
3m
Crystal was grown by chemical vapor transport technique with halogen gas.
I2 gas  2H
Cl2 gas  3R
Size of crystal
~1x1mm2
R. Suzuki et al.

## Slide 22: APRES measurement (@ The Univ. Tokyo)
Kinetic energy: Ekin
Emission angle: θ
Photoelectrons
Binding energy: EB
Momentum :k
Band dispersions
Sample is cleaved in situ at R. T.
hn = 21.2 (He I a) eV and 40.8 eV (He II)
(He discharge lamp)
T = 15 K
DE : 10 meV (He I a), 20 meV (He II)
In vacuum
In solids
Work function
M. Sakano et al.

## Slide 23: 3R-MoS2 : Band structure
Projected
2D-Brillouin
zone
K
K
G
G
K’
K
ky
kx
kz
ARPES image along G-K
K
K’
G
1st-principles calculation (R. Akashi)
Good agreement with calculation
hn = 40.8 eV
hn = 21.2 eV
Fermi surface
Fermi surface
hn = 21.2 eV
VB; VBM at G, valleys at K (K’)
CB; CBM valleys at K (K’) and/or ~0.5G-K(K’)

## Slide 24
Calculations
Valence band top at K
Spin-split
2 bands
Spin-
degenerate
4 bands
3R- and 2H-MoS2; Top of valence bands at K-point
3R-
MoS2
2H-
MoS2
ARPES images
G
K’
K
ky
kx
kz
3R-MoS2; Band splitting
at the top of K-point ~0.14 eV
0.14
eV
0.17
eV
x
z

## Slide 25: Spin-APRES measurement @HiSOR BL-9B ESPRESSO machine
Sample is cleaved in situ at R. T.
hn = 20 eV (p-polarized light)
T = 20 K
DE : 20-25 meV
Dq : ±0.75 deg
Spin component projected on the crystal axes
Spin component observed by spin detector

## Slide 26
3R-MoS2; Spin-splitting at K-point
Contour of valence band top
E-EF
= -2.3 eV
SARPES spectra/spin-polarizations
Spin-splittings at BZ corners
Centrosymmetric
2H-MX2
(P63 /mmc)
(Sx, Sz)
Spin-polarization; |Pz|~1

## Slide 27
3R-MoS2; Spin-splitting at K-point
ARPES / SARPES image
1ML-MX2 k・p effective Hamiltonian for VB top around K-point
D. Xiao et al., PRL 108, 196802 (2012).
“Zeeman-type” spin-splitting at K-point
Pauli matrix for spin
τ = ±1: Valley index

## Slide 28
SARPES spectra @K, K’
E-EF
= -2.3 eV
3R-MoS2; Spin-splitting at K- and K’-point
Sz flipping
M
Sz flipping; K ↔ K’
cf. 1ML-MX2 k・p effective Hamiltonian for VB top around K-point
D. Xiao et al., PRL 108, 196802 (2012).
Pauli matrix for spin
τ = ±1: Valley index
Coupled degrees of freedom
Spin + Valley in bulk
Contour of valence band top

## Slide 29: Comparison to 2H system
Centrosymmetric
2H-MX2
(P63 /mmc)
(Sx, Sz)
Calculated spin polarization Sz
3R-MoS2
2H-MoS2
Surface contribution; ruled out

## Slide 30
In 3R-MoS2…
Spin-splitting in bulk
Surface contribution; ruled out
Spin-valley coupling; Pz~±1 @K, K’
3R-MoS2
(R3m)
1ML MoS2
(P6m2)
Summary
3R-MoS2
(R3m)
2H-MX2
(P63 /mmc)
K
K’
G
E
3R-polytype TMDC will enrich
device fabrications and valley/spin related physics.
Results are published in Nat. Nanotech. 9, 611 (2014).

## Slide 31: Coworkers
Au/Ni(110) Sample fabrication, characterization STM and Spin-ARPES
T. Warashina
M. Nurmamat
MoS2 Spin-ARPES
K. Miyamoto
K. Kuroda
A. Kimura
H. Namatame
M. Taniguchi
＜Spin group@ HiSOR, Hiroshima Univ.＞
＜Financial support＞
MERIT, ALPS, GCOE
JSPS, Kiban B 19340078
JSPS, Kiban A 23244066
＜MoS2 project @ Univ. Tokyo＞
Sample fabrication and characterization
R. Suzuki
Y. J. Zhang
D. Morikawa
Y. Iwasa
ARPES & Spin-ARPES
M. Sakano
K. Ishizaka
K. Yaji
Harasawa
Calculation
R. Akashi
R. Arita
Thank you for your kind attention!